TP-P110

RUTILE TITANIUM DIOXIDE | FILM MASTERBATCH

TIOVAR TP-P110 is a rutile titanium dioxide pigment described by the supplier as produced by a chlorination process with special surface treatment. It is intended for formulation evaluation in film products.

| Applications Formulation evaluation in PET film masterbatch Formulation evaluation in PE, PP and other polyolefin masterbatches Supplier-reported Key Features Excellent dispersion Excellent thermal stability High hiding power and high tinting strength Excellent processing property |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 96. Rutile content, %; 99.9. L*; 98.2. b*; 1.70. Specific gravity, g/cm3; 4.1. Volatile (during packing), %; 0.1. Carbon black undertone (CBU); 17.0. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes excellent processing property for this film masterbatch grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE