TP-PA110

RUTILE TITANIUM DIOXIDE | PAPER

TIOVAR TP-PA110 is a chloride-process rutile titanium dioxide pigment described by the supplier as having special surface treatment. It is intended for formulation evaluation in paper products.

| Applications Formulation evaluation in plain paper, grainy paper and printed decorative paper Formulation evaluation in decoration paper, Bible paper, dictionary paper and paperboard Supplier-reported Key Features High whiteness Super UV stability Outstanding opacity and retention performance Excellent dispersion performance in alkaline water systems |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 90. Rutile content, %; 99.9. L* dry; 99.3. b*; 1.00. Specific gravity, g/cm3; 4.0. pH; 7.0. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes excellent dispersion performance in alkaline water systems for this paper grade. Verification in the intended formulation is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE