TP-C050

RUTILE TITANIUM DIOXIDE | ELECTROPHORETIC & GENERAL COATINGS

TIOVAR TP-C050 is a chloride-process rutile titanium dioxide pigment described by the supplier as specially treated, with excellent optical properties and lower ion content. It is intended for formulation evaluation in electrophoretic paints and general interior coatings.

| Applications Formulation evaluation in electrophoretic primers and the cited secondary and finishing electrophoretic coating systems Formulation evaluation in industrial electrophoretic coatings for household appliances, electromechanical equipment, hardware and electronics Formulation evaluation in interior architectural paints and industrial coatings Formulation evaluation in powder paints Formulation evaluation in water-borne and solvent-borne inks Supplier-reported Key Features High whiteness High gloss High hiding power Low ion content |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 95. Rutile content, %; 99.9. L*; 98.4. b*; 1.80. Specific gravity, g/cm3; 4.1. pH; 7.5. Carbon black undertone (CBU); 13.0. Oil absorption, g/100 g; 18. Mean particle size, micrometres; 0.28. Electrical resistivity, Ω•m; 500. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes lower ion content for this coating grade. Verification in the intended formulation is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE