TP-I200

RUTILE TITANIUM DIOXIDE | WATER-BASED PRINTING INKS

TIOVAR TP-I200 is a rutile titanium dioxide pigment made by the chloride process and given special surface treatment. The supplier describes it for water-based inks and other fields, with dry hiding power and resistance to UV. It is intended for formulation evaluation in printing inks requiring high weather resistance.

| Applications Formulation evaluation in water-based printing inks requiring high weather resistance Supplier-reported Key Features Ultra-high dry hiding power Excellent weather resistance, especially resistance to UV color change Excellent water dispersibility |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 77. Rutile content, %; 99.9. L*; 98.3. b*; 1.80. Specific gravity, g/cm3; 3.6. Oil absorption, g/100 g; 35. pH; 1.6. Carbon black undertone (CBU); 11.0. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes dry hiding power and resistance to UV for this ink grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE