TP-P200

RUTILE TITANIUM DIOXIDE | EXTERIOR PLASTICS

TIOVAR TP-P200 is a chloride-process rutile titanium dioxide pigment described by the supplier as using special surface treatment technology for plastic systems. It is intended for formulation evaluation in exterior plastics.

| Applications Formulation evaluation in high-durability uPVC extruded products, such as profiles, plates and exterior furniture Formulation evaluation in PVC calendering films, such as advertising plastic sheeting Formulation evaluation in weather-resistant color masterbatches Supplier-reported Key Features High weatherability Excellent processing property High color fastness High anti-chalking |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 92. Rutile content, %; 99.9. L*; 98.2. b*; 1.70. Specific gravity, g/cm3; 4.0. Volatile (during packing), wt%; 0.3. Acid solubility; 0.50. Carbon black undertone (CBU); 13.0. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes excellent dispersibility and processing rheology in plastic systems. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE