TP-P300

RUTILE TITANIUM DIOXIDE | ENGINEERING PLASTICS

TIOVAR TP-P300 is a chloride-process rutile titanium dioxide pigment described by the supplier as having special surface treatment. It is intended for formulation evaluation in polycarbonate systems and polyester applications.

| Applications Formulation evaluation in polycarbonate Formulation evaluation in polycarbonate masterbatch Formulation evaluation in engineering plastics such as PET, PA and ABS Formulation evaluation in PO masterbatch, its copolymers and plastics Supplier-reported Key Features Strong anti-degradation ability Excellent temperature resistance Good dispersibility Bluish undertone High hiding power and high tinting strength Excellent processing property |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 95. Rutile content, %; 99.9. L*; 98.2. b*; 1.55. Specific gravity, g/cm3; 4.1. Oil absorption, g/100 g; 14. Volatile (during packing), %; 0.1. Carbon black undertone (CBU); 17.0. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes excellent processing property for this engineering-plastics grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE