TP-C200

RUTILE TITANIUM DIOXIDE | HIGH-PVC ARCHITECTURAL COATINGS

TIOVAR TP-C200 is a rutile titanium dioxide pigment made by the chloride process and given special surface treatment. The supplier describes it for high-PVC architectural coatings and dry hiding performance. It is intended for formulation evaluation in architectural matte or flat coatings, including systems above the critical pigment volume concentration (CPVC).

| Applications Formulation evaluation in interior and exterior architectural coatings Formulation evaluation in high-hiding matte or flat coatings with pigment volume concentration above the critical pigment volume concentration (CPVC) Supplier-reported Key Features Ultra-high dry hiding power Excellent weather resistance Excellent water dispersibility High oil absorption |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 78. Rutile content, %; 99.9. L*; 98.3. b*; 1.80. Mean particle size, micrometres; 0.50. Oil absorption, g/100 g; 36. pH; 9.5. Carbon black undertone (CBU); 9.0. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes high-quality dry hiding power for this high-PVC architectural coating grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE