TP-S100

RUTILE TITANIUM DIOXIDE | SOLAR FILM

TIOVAR TP-S100 is a chloride-process rutile titanium dioxide pigment described by the supplier as having special surface treatment. It is intended for formulation evaluation in photovoltaic white films and plastic applications requiring high UV resistance.

| Applications Formulation evaluation in EVA photovoltaic white film Formulation evaluation in POE photovoltaic white film Formulation evaluation in plastics requiring high UV resistance Supplier-reported Key Features High whiteness Excellent UV resistance and yellowing resistance Good dispersibility Excellent processing property |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 89. Rutile content, %; 99.9. Carbon black undertone (CBU); 10.0. L*; 98.3. b*; 1.85. Specific gravity, g/cm3; 4.0. Volatile (content at packing), wt %; 0.3. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes excellent processing property for this solar-film grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE