TP-C400

RUTILE TITANIUM DIOXIDE | ULTRA-HIGH WEATHERABILITY COATINGS

TIOVAR TP-C400 is a chloride-process rutile titanium dioxide pigment. The supplier describes special inorganic and organic surface treatment and ultra-high weather resistance for this grade. It is intended for formulation evaluation where durability, weather resistance, gloss, hiding power, dispersibility, chalk resistance and color retention are required.

| Applications Formulation evaluation in automotive OEM and refinishing coatings Formulation evaluation in marine paint and aerospace coatings Formulation evaluation in exterior and industrial coatings Supplier-reported Key Features High durability High gloss High hiding power Excellent chalk resistance and color retention performance Good dispersibility |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 91. Rutile content, %; 99.9. L*; 98.3. b*; 1.80. Acid solubility; 0.40. Specific gravity; 4.0. Mean particle size, micrometres; 0.30. pH; 8.0. Carbon black undertone (CBU); 13.0. Oil absorption, g/100 g; 20. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively reports good dispersibility. Verification in the formulation is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE