TP-C310

RUTILE TITANIUM DIOXIDE | WATERBORNE COATINGS

TIOVAR TP-C310 is a chloride-process rutile titanium dioxide pigment. The supplier describes a special surface treatment for this grade. It is intended for formulation evaluation where durability, weather resistance, gloss, hiding power, dispersibility, color retention, water dispersibility and storage stability are required.

| Applications Formulation evaluation in automotive OEM and water-based automotive topcoats, component paints and refinishing coatings Formulation evaluation in water-soluble resin industrial coatings Formulation evaluation in exterior coatings requiring high weather resistance Supplier-reported Key Features High durability High gloss High hiding power Chalk resistance Excellent water dispersibility and storage stability |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 92. Rutile content, %; 99.9. L*; 98.4. b*; 1.80. Acid solubility; 0.40. Mean particle size, micrometres; 0.30. pH; 6.5. Carbon black undertone (CBU); 10.5. Oil absorption, g/100 g; 20. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively reports excellent water dispersibility and storage stability. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE