TP-H100

RUTILE TITANIUM DIOXIDE | HIGH-PURITY FUNCTIONAL APPLICATIONS

TIOVAR TP-H100 is a high-purity titanium dioxide grade described by the supplier as being produced by a vapor-phase oxidation method. The supplier reports high purity, low impurity content, narrow particle size distribution, good dispersion and stable quality between batches. It is intended for formulation evaluation in high-purity functional applications.

| Applications Formulation evaluation in electronic ceramics including MLCC, PTC, VDR and soft ferrite Formulation evaluation in optical glass and battery applications Formulation evaluation in cosmetics, medicine and special metallurgy applications Supplier-reported Key Features High purity, low impurity content and stable quality High dielectric constant and excellent electrical properties |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 99.97. Rutile content, %; 99. Specific surface area, m2/g; <6; 6-8; 8-10. Volatile matter, %; 0.1. Al, %; 0.0020. Fe, %; 0.0010. K, %; 0.0001. Na, %; 0.0050. P, %; 0.0005. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier reports good dispersion. Formulation-specific viscosity must be verified. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. The supplier table presents three specific-surface-area entries without variant labels; values are reproduced without assigning them to subgrades/variants. Product suitability must be evaluated in the intended formulation. Legal/contact details, SDS/COA issuer and packaging remain pending and are not for public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE