TP-P320

RUTILE TITANIUM DIOXIDE | ENGINEERING PLASTICS

TIOVAR TP-P320 is a chloride-process rutile titanium dioxide pigment described by the supplier as having special surface treatment. It is intended for formulation evaluation in high-reflective polycarbonate systems and engineering-plastics applications with high-reflection requirements.

| Applications Formulation evaluation in high-reflective polycarbonate Formulation evaluation in high-reflective polycarbonate masterbatch Formulation evaluation in engineering plastics with high-reflection requirements Supplier-reported Key Features High whiteness High reflectance Good dispersibility Bluish undertone Excellent processing property Outstanding anti-degradation ability |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 91. Rutile content, %; 99.9. L*; 98.4. b*; 1.60. Specific gravity, g/cm3; 4.0. Oil absorption, g/100 g; 17. Volatile (during packing), %; 0.3. Carbon black undertone (CBU); 13.5. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes excellent processing property for this high-reflection engineering-plastics grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE