TP-PA100

RUTILE TITANIUM DIOXIDE | PAPER

TIOVAR TP-PA100 is a chloride-process rutile titanium dioxide pigment described by the supplier as specially treated. It is intended for formulation evaluation in high-quality decorating paper and other cited paper products.

| Applications Formulation evaluation in decorating paper, Bible paper, dictionary paper and paperboard Supplier-reported Key Features Excellent UV stability Marvelous dispersibility in water High hiding power High whiteness |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 90. Rutile content, %; 99.9. L* dry; 99.1. b*; 1.20. Specific gravity, g/cm3; 4.0. pH; 7.5. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes marvelous dispersibility in water for this paper grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE