TP-C110

RUTILE TITANIUM DIOXIDE | MULTI-PURPOSE COATINGS

TIOVAR TP-C110 is a chloride-process rutile titanium dioxide pigment described by the supplier as a multi-purpose grade. It is intended for formulation evaluation in solvent and water-based systems, including architectural, industrial and decorative coatings, with cited paper applications.

| Applications Formulation evaluation in interior and exterior flat and semi-gloss architectural paints, industrial coatings and decorative coatings, especially water-borne systems Formulation evaluation in Bible paper, decorating paper and paperboard production Supplier-reported Key Features Neutral tint High hiding power High whiteness Good durability |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 93. Rutile content, %; 99.9. L*; 98.4. b*; 1.80. Specific gravity, g/cm3; 4.0. Oil absorption, g/100 g; 20. Mean particle size, micrometres; 0.30. Acid solubility; 1.6. Carbon black undertone (CBU); 13.0. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes performance in solvent and water-based systems for this multi-purpose grade. Verification in the intended formulation is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE