TP-I100

RUTILE TITANIUM DIOXIDE | PRINTING INKS AND HIGH-HIDING APPLICATIONS

TIOVAR TP-I100 is a chloride-process rutile titanium dioxide pigment. The supplier describes this grade as a special titanium dioxide for solvent-based and water-based inks. It is intended for formulation evaluation where neutral tint, whiteness, hiding power, dispersibility and low oil absorption are required.

| Applications Formulation evaluation in inkjet inks Formulation evaluation in water-based inks Formulation evaluation in correction fluids Formulation evaluation in color pastes Formulation evaluation in coatings with high hiding power requirements Supplier-reported Key Features Neutral tint High whiteness and high hiding power Outstanding dispersibility Low oil absorption |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 98. Rutile content, %; 99.9. L*; 98.4. b*; 1.80. Specific gravity, g/cm3; 4.0. Carbon black undertone (CBU); 12.5. Oil absorption, g/100 g; 14. Mean particle size, micrometres; 0.35. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier reports outstanding dispersibility and low oil absorption. Formulation-specific viscosity must be verified. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE