TP-P100

RUTILE TITANIUM DIOXIDE | POLYOLEFIN COLOR MASTERBATCH

TIOVAR TP-P100 is a chloride-process rutile titanium dioxide pigment described by the supplier as receiving special inorganic and organic surface treatment. It is intended for formulation evaluation in polyolefin color masterbatch and plastics.

| Applications Formulation evaluation in polyolefin masterbatch Formulation evaluation in engineering plastics such as PE, PP and ABS Formulation evaluation in PS, its copolymers and rubber Supplier-reported Key Features Bluish undertone High hiding power and high tinting strength Easy dispersion in many polymers Excellent processing performance |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 96. Rutile content, %; 99.9. Carbon black undertone (CBU); 17.5. L*; 98.3. b*; 1.70. Specific gravity, g/cm3; 4.1. Volatile (content at packing), wt%; 0.1. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier qualitatively describes excellent processing performance for this plastics grade. Formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE