TP-C120

RUTILE TITANIUM DIOXIDE | WATER-BASED EMULSION PAINT

TIOVAR TP-C120 is a chloride-process rutile titanium dioxide pigment described by the supplier as having zirconium-aluminum and special organic surface treatment. It is intended for formulation evaluation in water-based interior and exterior wall emulsion paints.

| Applications Formulation evaluation in water-based interior wall emulsion paint Formulation evaluation in water-based exterior wall emulsion paint Supplier-reported Key Features Bluish tone High gloss High durability High hiding power |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 95. Rutile content, %; 99.9. Dry L*; 99.4. Dry b*; 1.00. Specific gravity, g/cm3; 4.1. pH; 7.5. Carbon black undertone (CBU); 14.0. Oil absorption, g/100 g; 17. Mean particle size, micrometres; 0.27. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier uses only the qualitative phrase 'relatively low viscosity' for water-based emulsion paint. No result or method is supplied; formulation-specific verification is required. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE