TP-U100

RUTILE TITANIUM DIOXIDE | MULTIPURPOSE COATINGS, INKS AND PLASTICS

TIOVAR TP-U100 is a chloride-process rutile titanium dioxide pigment described by the supplier as specially surface-treated and multifunctional. It has an excellent particle size distribution and is intended for formulation evaluation in coatings, printing inks and plastics.

| Applications Formulation evaluation in interior and exterior architectural coatings Formulation evaluation in automotive OEM and refinishing, coil, anticorrosion, decorative and powder coatings Formulation evaluation in letterpress, offset and intaglio printing inks Formulation evaluation in engineering plastics, masterbatch and profiles Supplier-reported Key Features Bluish tone High gloss High durability Multifunction |  | Reported Technical Data Property; Reported Value. TiO2 content, %; 95. Rutile content, %; 99.9. L*; 98.4. b*; 1.75. Specific gravity, g/cm3; 4.1. pH; 7.5. Carbon black undertone (CBU); 14.0. Oil absorption, g/100 g; 17. Mean particle size, micrometres; 0.27. |
| --- | --- | --- |

| Performance & Packaging Viscosity The supplier describes an excellent particle size distribution. Formulation-specific viscosity must be verified. Packaging Packaging is not stated in the supplier TDS. The supplied packaging artwork is a concept mockup only and is not approved evidence of pack size, label text, or legal attribution. |  | Safety / SDS Status An aligned SDS was not provided for this draft. Confirm the supplied-product identifier, issuing entity, emergency contact, and revision before external use. |
| --- | --- | --- |

Supplier-reported values reproduce the primary supplier TDS. The source does not state test methods, tolerances, or whether values are typical or specification limits. Product suitability must be evaluated in the intended formulation. Legal attribution, company contacts, SDS/COA issuer and packaging details remain unconfirmed and are withheld from public use.

Release Status Pending user confirmation before public use: brand owner; manufacturer / manufactured-for / distributor; SDS and COA issuer; packaging label entity; company contact details; trademark status.

DRAFT - NOT APPROVED FOR PUBLIC USE